**************************************************************************

- Referee: Hector Somacal

- Author: C. R. Appoloni, M. S. Blonski, P. S. Parreira and L. A. C. Souza

Title: Pigments Elementary Chemical Composition Study of a Gainsborough Attributed Painting Employing a Portable X-Rays Fluorescence System

Type of presentation:  Plenary       ( )

Oral          ( )

Poster        (x)

- 1. Please summarize your assessment of the paper:

YES   MAYBE   NO

Is the paper scientifically sound and not misleading?   (x)    ( )   ( )

Is the paper well organized and clearly written?        (x)    ( )   ( )

- 2.  Please evaluate quality of Research and Presentation:

(  ) Excellent (  )

(  ) Good      (  )

(  ) Average   ( x)

(  ) Marginal  (  )

(  ) Poor      (  )

- 3.  Recommendation -

(  ) Publish without change (please give reasons in report).

(  ) Publish after authors have considered the optional revisions mentioned

in the report.

( x ) Publish after authors have made the revisions mentioned in the report.

(I do not need to see the manuscript again.)

(  ) Revisions are necessary. Return to me on resubmittal.

(  ) Do not publish; see report.

************************************************************************

begin_report (use as much space as is needed):

There are three comments to do:

- In Materials and Methods, the authors did not mention the use of Ar that is present in all spectra, however the energies of Ar K-lines are equal to the Ag (anode) L-lines. This point must be clarified.

As the measures were accomplished in air, the line of Ar will always be present. On the other hand, due to the anode of the tube to be of Ag, the line L-lines will be overlap with K of the Ar, what is not problem, because the presented analysis doesn't involve the lines of these elements. (These comments were inserted in the text in the paper)

- In Results and Discussion, the authors report the presence of S and Hg in the Face region associated to HgS (vermilion). Figure 5 shows the presence of S in the Face region clearly, but Hg is not evident in this spectrum. How did the authors conclude about the prsence of Hg?

The area of the peak of  Hg was extracted employing the sofware AXIL , it doesn't appear clearly in the spectrum of the figure 5 due to the fund of the spectrum, but it can be verified in the Table 1 that the liquid area of this element was determined with just 2,7% of deviation, confirming its presence in the spectrum. (The table 1 was inserted in the paper)

end_report

************************************************************************